Fluence Threshold Parameters

ZnSe | ZnS | BaF2 | NaCl | Ge | IRG207 | KRS-5 | CdTe

Standalone threshold-fluence comparison. This reference does not alter the Keldysh photoionization, avalanche-ionization, or carrier-density models.

Shared model and unit checks

F_th = [3 n_a λ / (16 π)] (ε_b + E_g)

| Quantity | Required internal form | Conversion / rule |
| --- | --- | --- |
| Atomic density, n_a | m^-3 | n_a = N_atoms ρ N_A / M; use total atomic density. |
| Wavelength, λ | m | λ_m = λ_µm × 10^-6. |
| ε_b and E_g | J | E_J = E_eV × 1.602176634 × 10^-19. |
| Threshold fluence | J/m² | Report J/cm² using F_th(J/cm²) = 10^-4 F_th(J/m²). |
| Comparison | dimensionless | F0/F_th compares experimental peak fluence with the threshold. |

Use a cohesive/binding energy on the same per-atom basis as the total atomic number density. Do not mix fluence F0 with peak intensity I0.

Variable definitions / code key

| Code variable | Symbol | Definition | Role / unit |
| --- | --- | --- | --- |
| mass_density_kg_m3 | ρ | Material mass density | INPUT; kg/m³ |
| molar_mass_kg_mol | M | Molar mass | INPUT; kg/mol |
| atoms_per_formula_unit | N_atoms | Atoms per formula unit | INPUT; 2 for ZnSe/ZnS, 3 for BaF2 |
| binding_energy_ev_per_atom | ε_b | Cohesive/binding energy | INPUT; eV/atom |
| bandgap_ev | E_g | Bandgap energy | INPUT; eV |
| wavelength_um | λ | Vacuum wavelength | INPUT; µm |
| F0_jcm2 | F0 | Experimental peak fluence | INPUT; J/cm² |
| n_a_m3 | n_a | Total atomic number density | DERIVED; m⁻³ |
| Fth_jm2 / Fth_jcm2 | F_th | Threshold fluence | OUTPUT; J/m² and J/cm² |
| F0_over_Fth | F0/F_th | Experimental-to-threshold ratio | OUTPUT; dimensionless |

I0 and pulse duration τ are not inputs to F_th; use them only in the separate intensity-based PI/II model.

ZnSe

INPUT

| Parameter | Input / derived value | Unit or basis |
| --- | --- | --- |
| ρ | 5270 | kg/m³; source-verified bulk density |
| M_ZnSe | 0.14434 | kg/mol |
| N_atoms | 2 | Zn + Se per formula unit |
| ε_b | 2.6 | eV/atom; cohesive/binding energy |
| E_g | 2.7 | eV |

EXPERIMENTAL PEAK-FLUENCE INPUT

| Condition | λ (µm) | F0 (J/cm²) |
| --- | --- | --- |
| NIR | 0.8 | 0.15 |
| LWIR | 9.2 | 0.83 |

OUTPUT

| Quantity | Value | Meaning |
| --- | --- | --- |
| F_th | Pending input | Requires ρ and ε_b. |
| F0/F_th | Pending input | Dimensionless comparison. |

Complete the two INPUT fields before reporting a quantitative ZnSe threshold.

ZnS

INPUT

| Parameter | Input / derived value | Unit or basis |
| --- | --- | --- |
| ρ | 4090 | kg/m³; source-verified bulk density |
| M_ZnS | 0.09744 | kg/mol |
| N_atoms | 2 | Zn + S per formula unit |
| ε_b | 3.1 | eV/atom; cohesive/binding energy |
| E_g | 3.6 | eV |

EXPERIMENTAL PEAK-FLUENCE INPUT

| Condition | λ (µm) | F0 (J/cm²) |
| --- | --- | --- |
| NIR | 0.8 | 0.170 |
| LWIR | 9.2 | 1.19 |

OUTPUT

| Quantity | Value | Meaning |
| --- | --- | --- |
| F_th | Pending input | Requires ρ and ε_b. |
| F0/F_th | Pending input | Dimensionless comparison. |

Complete the two INPUT fields before reporting a quantitative ZnS threshold.

BaF2

INPUT

| Parameter | Input / derived value | Unit or basis |
| --- | --- | --- |
| ρ | 4890 | kg/m³ |
| M_BaF2 | 0.175323806 | kg/mol |
| N_atoms | 3 | Ba + 2F per formula unit |
| ε_b | 6.0133 | eV/atom = 18.04 eV per formula unit / 3 |
| E_g | 10.6 | eV |

EXPERIMENTAL PEAK-FLUENCE INPUT

| Condition | λ (µm) | F0 (J/cm²) |
| --- | --- | --- |
| NIR | 0.8 | 0.9441 |

OUTPUT

| Quantity | Value | Meaning |
| --- | --- | --- |
| n_a | 5.0390 × 10^28 | m^-3; total atomic density. |
| F_th | 0.6404 | J/cm² (6.4040 × 10^3 J/m²). |
| F0/F_th | 1.4743 | Experimental F0 is 1.4743 times the model threshold. |

BaF2 uses cohesive/binding energy, not the ionic lattice energy. F0 is the measured elliptical-Gaussian peak fluence.

NaCl

INPUT

| Parameter | Input / derived value | Unit or basis |
| --- | --- | --- |
| ρ | 2165 | kg/m³ |
| M_NaCl | 0.058443 | kg/mol |
| N_atoms | 2 | Na + Cl per formula unit |
| ε_b | 3.2 | eV/atom |
| E_g | 8.5 | eV |

EXPERIMENTAL PEAK-FLUENCE INPUT

| Condition | λ (µm) | F0 (J/cm²) |
| --- | --- | --- |
| NIR | 0.8 | 0.392289 |

OUTPUT

| Quantity | Value | Meaning |
| --- | --- | --- |
| n_a | 4.4618 × 10^28 | m^-3; total atomic density. |
| F_th | 0.3993 | J/cm² (3.9934 × 10^3 J/m²). |
| F0/F_th | 0.9823 | Experimental F0 is 0.9823 times the model threshold. |

NaCl uses cohesive energy on a per-atom basis. F0 = 0.392289 J/cm² is from the 150 µJ pulse with the BaF2 elliptical beam diameters.

Ge

INPUT

| Parameter | Input / derived value | Unit or basis |
| --- | --- | --- |
| ρ | 5323 | kg/m³; NIST bulk density |
| M_Ge | 0.072630 | kg/mol; elemental Ge |
| N_atoms | 1 | one Ge atom per elemental formula unit |
| ε_b | 3.85 | eV/atom; not specified in the Ge Keldysh input |
| E_g | 0.660 | eV; 300 K indirect-gap input |

EXPERIMENTAL PEAK-FLUENCE INPUT

| Condition | λ (µm) | F0 (J/cm²) |
| --- | --- | --- |
| NIR | 0.8 | 0.0485 |

OUTPUT

| Quantity | Value | Meaning |
| --- | --- | --- |
| n_a | 4.4136 × 10^28 | m^-3; total atomic density |
| F_th | Pending ε_b | Cannot calculate without cohesive/binding energy per atom |
| F0/F_th | Pending ε_b | Dimensionless comparison |

Ge uses NIST density and the elemental molar mass. The 0.660 eV value is the Keldysh indirect-gap input. Supply a verified cohesive/binding energy in eV/atom before reporting F_th.

IRG207

INPUT

| Parameter | Input / derived value | Unit or basis |
| --- | --- | --- |
| ρ | 4470 | kg/m³; SCHOTT IRG 24 proxy |
| M_proxy | 7.671714 | kg/mol for Ge10As40Se50 (100-atom pseudo-formula) |
| N_atoms | 100 | Ge10As40Se50 pseudo-formula |
| ε_b | Pending | eV/atom; no verified IRG207 value |
| E_g | 1.70 | eV; provisional optical-gap input |

EXPERIMENTAL PEAK-FLUENCE INPUT

| Condition | λ (µm) | F0 (J/cm²) |
| --- | --- | --- |
| NIR | 0.8 | 0.0485 |

OUTPUT

| Quantity | Value | Meaning |
| --- | --- | --- |
| n_a | 3.5089 × 10^28 | m^-3; IRG 24 proxy total atomic density |
| F_th | Pending ε_b | Cannot calculate without cohesive/binding energy per atom |
| F0/F_th | Pending ε_b | Dimensionless comparison |

IRG207 is represented by the SCHOTT IRG 24 proxy Ge10As40Se50 with density 4.47 g/cm³. Confirm the IRG207 batch/composition and provide ε_b before using the threshold quantitatively.

KRS-5

INPUT

| Parameter | Input / derived value | Unit or basis |
| --- | --- | --- |
| ρ | 7370 | kg/m³; ISP/Edmund KRS-5 material data |
| M_nominal | 0.312484 | kg/mol; nominal 40 mol% TlBr + 60 mol% TlI |
| N_atoms | 2 | one Tl plus one mixed-halide site |
| ε_b | Pending | eV/atom; no verified KRS-5 value |
| E_g | 2.50 | eV; provisional Keldysh placeholder |

EXPERIMENTAL PEAK-FLUENCE INPUT

| Condition | λ (µm) | F0 (J/cm²) |
| --- | --- | --- |
| NIR | 0.8 | 0.0606 |

OUTPUT

| Quantity | Value | Meaning |
| --- | --- | --- |
| n_a | 2.8407 × 10^28 | m^-3; nominal-composition total atomic density |
| F_th | Pending ε_b | Cannot calculate without cohesive/binding energy per atom |
| F0/F_th | Pending ε_b | Dimensionless comparison |

KRS-5 is treated as nominal 40 mol% TlBr and 60 mol% TlI with density 7.37 g/cm³. The exact specimen composition and the provisional 2.50 eV gap must be confirmed; ε_b is still required.

CdTe

INPUT

| Parameter | Input / derived value | Unit or basis |
| --- | --- | --- |
| ρ | 5850 | kg/m³; NIST compound density |
| M_CdTe | 0.240011 | kg/mol |
| N_atoms | 2 | Cd + Te per formula unit |
| ε_b | 2.2 | eV/atom; not specified in the CdTe Keldysh input |
| E_g | 1.5125 | eV; approximately 300 K direct gap |

EXPERIMENTAL PEAK-FLUENCE INPUT

| Condition | λ (µm) | F0 (J/cm²) |
| --- | --- | --- |
| NIR | 0.8 |  |

OUTPUT

| Quantity | Value | Meaning |
| --- | --- | --- |
| n_a | 2.9357 × 10^28 | m^-3; total atomic density |
| F_th | Pending ε_b | Cannot calculate without cohesive/binding energy per atom |
| F0/F_th | Pending F0 and ε_b | No experimental surface fluence is entered |

CdTe uses NIST density, molar mass, and the 1.5125 eV Keldysh gap input. Both a verified cohesive/binding energy per atom and an experimental surface fluence are required for the full comparison.