# Keldysh Parameter of GaAs: Formula, Symbol Values, and Reliable Sources

Reference diagnostic example at 800 nm and a peak intensity of 1.00×10¹³ W/cm²

# 1. Formula and Interpretation

γ = (ω/e) √[(mᵣ e c n ε₀ E_g)/I]

Here, E_g is entered in eV and e converts it to joules; I is in W/m². This document and the script follow the source-paper convention E = √[I/(cnε₀)], so γ contains I, not 2I, in the denominator. For GaAs at 800 nm, hν = 1.550 eV exceeds the 300 K direct gap E_g = 1.424 eV. One-photon interband absorption is therefore allowed. The γ values below are diagnostic values only, not a complete Ti:Sa-on-GaAs excitation or damage model.

# 2. Numerical Value, Range, and Source for Every Symbol

| Symbol | Meaning | Value or Range Used for GaAs | Unit | Source and Cautionary Note |
| --- | --- | --- | --- | --- |
| γ | Keldysh parameter | Diagnostic reference value: 0.509 | Dimensionless | Calculated from the real-n diagnostic inputs below using the source-paper convention E = √[I/(cnε₀)]. Do not interpret it alone as the dominant excitation mechanism at 800 nm. |
| ω | Laser angular frequency, ω = 2πc/λ | 2.35456×10¹⁵ | rad·s⁻¹ | Calculated from λ = 800 nm and the exact value of c. |
| e | Elementary charge | 1.602176634×10⁻¹⁹ | C | Exact SI-defined value; NIST CODATA. |
| mᵣ | Γ electron–heavy-hole reduced mass | 0.0591 m₀ = 5.382×10⁻³² | kg | Derived from mₑ* = 0.067m₀ and mₕₕ* = 0.50m₀. Declare the band choice; this is not a universal scalar for all GaAs transitions. |
| c | Speed of light in vacuum | 299792458 | m·s⁻¹ | Exact SI-defined value; NIST CODATA. |
| n + iκ | Complex GaAs optical index (800 nm) | 3.682 + 0.069i | Dimensionless | The solver uses only n = 3.682 for its zero-D field conversion. κ must enter any propagation and linear-absorption model. |
| ε₀ | Vacuum permittivity | 8.8541878188×10⁻¹² | F·m⁻¹ | NIST CODATA recommended value. |
| E_g | GaAs direct Γ gap (300 K) | 1.424 | eV | Verify temperature and doping; hν(800 nm) = 1.550 eV > E_g. |
| I | Peak laser intensity | Reference: 1.00×10¹³ W/cm² = 1.00×10¹⁷ W/m² | W/m² | Experimental input. Derive from the actual focused pulse; do not use average power divided by area. |
| F₀ | Peak fluence | 0.022 | J/cm² | Experimental input; left blank because no fluence is specified. |
| a | 1/e² intensity radius along the first principal axis | 162.1 | µm | Experimental 1/e² intensity radius; left blank because it is not specified. If supplied from a diameter, use half of the full 1/e² intensity diameter. |
| b | 1/e² intensity radius along the second principal axis | 152.4 | µm | Experimental 1/e² intensity radius; left blank because it is not specified. If supplied from a diameter, use half of the full 1/e² intensity diameter. |
| λ | Laser vacuum wavelength | 800 nm = 8.00×10⁻⁷ m | m | Experimental input; a common Ti:Sapphire reference wavelength. |
| m₀ | Free-electron rest mass | 9.1093837139×10⁻³¹ | kg | NIST CODATA recommended value, used to express effective-mass ratios. |

# 3. Reproducible GaAs Optical-Index Input

GaAs is not transparent at the 800 nm Ti:Sapphire fundamental: 800 nm is shorter than the nominal band-edge wavelength λ_g = hc/E_g = 870.7 nm. The room-temperature bulk optical input used here is n + iκ = 3.682 + 0.069i.

For continuity with the BaF₂-style diagnostic calculation, the real part n = 3.682 is used in γ. In a physical simulation, retain κ = 0.069 (or the measured absorption coefficient α), surface reflectance, sample temperature, doping, and thickness; then propagate the depth-dependent intensity and include direct interband generation.

The Ti:sapphire center wavelength is an experimental input, not a GaAs material constant. Pulse duration does not enter γ after the peak intensity is known; use the actual temporal and spatial pulse shape when converting from fluence or pulse energy to I₀.

# 4. Reference Numerical Calculation

| Parameter | Reference Value | Note |
| --- | --- | --- |
| λ | 800 nm | Specified diagnostic laser wavelength |
| ω | 2.35456×10¹⁵ rad·s⁻¹ | From 2πc/λ |
| n + iκ | 3.682 + 0.069i | γ uses n = 3.682 only; κ and α are required for the physical 800 nm model |
| E_g | 1.424 eV | 300 K direct gap |
| mᵣ | 0.0591 m₀ | Γ-electron / heavy-hole reference mass |
| I | 1.00×10¹³ W/cm² | Specified peak intensity |
| F₀ | 0.022 | Experimental input; left blank because no fluence is specified. |
| a | 162.1 | Experimental 1/e² intensity radius; left blank because it is not specified. If supplied from a diameter, use half of the full 1/e² intensity diameter. |
| b | 152.4 | Experimental 1/e² intensity radius; left blank because it is not specified. If supplied from a diameter, use half of the full 1/e² intensity diameter. |
| γ | 0.509 (diagnostic) | One-photon absorption must be included |

Calculated diagnostic result: γ = 0.509 using the source-paper convention E = √[I/(cnε₀)]. Its numerical value is below one, but it must not be labelled a tunneling-dominated GaAs response at 800 nm, because direct one-photon absorption is energetically allowed and is omitted by the lossless Keldysh expression.

# 5. Sensitivity to Effective-Mass Uncertainty

| Assumed mₑ* / mₕₕ* | Derived mᵣ | Diagnostic γ | Interpretation |
| --- | --- | --- | --- |
| 0.063m₀ / 0.45m₀ | 0.0553m₀ | 0.492 | Diagnostic only; 800 nm has direct interband absorption |
| 0.067m₀ / 0.50m₀ | 0.0591m₀ | 0.509 | Reference input; diagnostic only |
| 0.067m₀ / 0.51m₀ | 0.0593m₀ | 0.510 | Diagnostic only; 800 nm has direct interband absorption |

The required mass is transition-specific. The reference uses the Γ-valley electron mass mₑ* = 0.067m₀ and heavy-hole mass mₕₕ* = 0.50m₀, giving mᵣ = (mₑ*mₕₕ*)/(mₑ*+mₕₕ*) = 0.0591m₀. Literature conventions and nonparabolicity produce modest variants; declare the chosen bands and masses in every calculation.

# 6. Peak-Intensity Scan (Diagnostic γ; 800 nm, n = 3.682, E_g = 1.424 eV)

| Peak Intensity (W/cm²) | Diagnostic γ | Physical Interpretation at 800 nm |
| --- | --- | --- |
| 1×10¹² | 1.610 | Linear interband absorption present; γ is supplementary |
| 1×10¹³ | 0.509 | Linear interband absorption present; γ is supplementary |
| 1×10¹⁴ | 0.161 | Linear interband absorption present; γ is supplementary |
| 1×10¹⁵ | 0.0509 | Linear interband absorption present; γ is supplementary |

# 7. References

• Ioffe Institute, NSM Archive, Gallium Arsenide: 300 K band structure and carrier-concentration tables. Reports E_g = 1.424 eV, Γ-electron mass 0.063m₀, heavy-hole mass 0.51m₀, and effective valence-band density of states 9.0×10¹⁸ cm⁻³.

• Vurgaftman, I., Meyer, J. R., & Ram-Mohan, L. R. (2001). Band parameters for III–V compound semiconductors. Journal of Applied Physics, 89, 5815–5875. Standard compilation for GaAs band and effective-mass parameters; values depend on convention and temperature.

• Aspnes, D. E., Kelso, S. M., Logan, R. A., & Bhat, R. (1986). Optical properties of AlₓGa₁₋ₓAs. Journal of Applied Physics, 60, 754–767. Room-temperature complex optical constants used to justify treating GaAs at 800 nm as absorbing rather than as a lossless dielectric.

• National Academies of Sciences, Engineering, and Medicine (2018). Opportunities in Intense Ultrafast Lasers. Ti:sapphire systems operate around a central wavelength of 800 nm; the actual laser spectrum and pulse duration remain experiment-specific inputs.

• NIST CODATA recommended values of the fundamental physical constants: e, c, ε₀, and m₀.

Concluding input note: use this document only as a traceable parameter specification and diagnostic γ calculation. For a Ti:sapphire 800 nm pulse in GaAs, include linear interband absorption from the outset. A transparent-medium Keldysh model becomes materially more defensible only at a sub-gap wavelength for the specified temperature and doping, with measured optical constants and band-specific effective masses.