# Ge Keldysh Input Parameter Specification

Reference example at 800 nm; SI conversion is applied internally.

# Scope and Material Identity

Material: Germanium (Ge). This sheet follows the BaF₂/NaCl input-document structure while retaining material-specific assumptions and limitations.

Parameter Status

# The reference calculation uses λ = 0.800 µm, I = 1.00 × 10¹³ W/cm², mᵣᵉ = 1.00 m₀, E_g = 0.66 eV (300 K indirect gap; the direct gap is approximately 0.80 eV), and Re(n) = 4.699.

| Symbol | Value | Unit | Definition / use | Status / source |
| --- | --- | --- | --- | --- |
| γ | 1.610866 | dimensionless | Keldysh parameter at I₀ | Calculated |
| c | 299792458 | m/s | Speed of light in vacuum | Exact SI |
| e | 1.602176634 × 10⁻¹⁹ | C | Elementary charge | Exact SI |
| ε₀ | 8.8541878128 × 10⁻¹² | F/m | Vacuum permittivity | Standard SI |
| mᵣᵉ | 1.00 | m₀ | Electron–hole reduced effective mass | Temporary project placeholder |
| n | 4.699 | dimensionless | Real refractive index at 800 nm | n + iκ = 4.699 + 0.259i at 0.800 µm for crystalline Ge near room temperature (Jellison tabulation). The calculation below uses only Re(n). |
| κ | 0.259 | dimensionless | Extinction coefficient at 800 nm | Not used in this zero-dimensional calculation |
| E_g | 0.66 | eV | Band-gap energy | 300 K indirect gap; the direct gap is approximately 0.80 eV |
| λ | 0.800 | µm | Vacuum wavelength | User-requested standard wavelength |
| ω | 2.354564e+15 | rad/s | Angular frequency, 2πc/λ | Calculated |
| I₀ | 1.00 × 10¹³ | W/cm² | Reference peak intensity | Independent scan input |
| F | Surface fluence | J/cm² | Surface fluence | User-supplied surface fluence; recorded as experiment input and not used to derive I in this sheet. |
| a | Beam-profile diameter along axis a | µm | Beam size along a | User-supplied 1/e² intensity beam diameter along the a axis. |
| b | Beam-profile diameter along axis b | µm | Beam size along b | User-supplied 1/e² intensity beam diameter along the b axis. |

At 800 nm, hν ≈ 1.550 eV exceeds both the indirect and direct gaps. Ge is absorbing; the zero-dimensional Keldysh result is diagnostic only because linear one-photon absorption, the imaginary index, reflection, and propagation are omitted.

# Reproducible Calculation and Optical-Index Basis

n + iκ = 4.699 + 0.259i at 0.800 µm for crystalline Ge near room temperature (Jellison tabulation). The calculation below uses only Re(n).

At 800 nm the photon energy is hν = 1.5498 eV. Optical constants and band-gap inputs must correspond to the actual sample temperature, composition, orientation, and batch whenever those variables are relevant.

Electric-field convention: E = √[2I/(c n ε₀)], so I = (1/2)c n ε₀E². The Keldysh expression below is kept consistent with the existing NaCl/BaF₂ documents and does not insert an additional factor of 2 into γ.

# Keldysh Parameter

| Input | Entered value | Implementation note |
| --- | --- | --- |
| Material | Germanium (Ge) | Material-specific standalone input |
| λ | 0.800 µm | Used to calculate ω |
| n + iκ | 4.699 + i(0.259) | Only Re(n) enters γ |
| E_g | 0.66 eV | 300 K indirect gap; the direct gap is approximately 0.80 eV |
| mᵣᵉ | 1.00 m₀ | Temporary project placeholder |
| I₀ | 1.00 × 10¹³ W/cm² | Converted to 1.00 × 10¹⁷ W/m² |
| F | Surface fluence J/cm² | User-supplied surface fluence; recorded as experiment input and not used to derive I in this sheet. |
| a | Beam-profile diameter along axis a µm | User-supplied 1/e² intensity beam diameter along the a axis. |
| b | Beam-profile diameter along axis b µm | User-supplied 1/e² intensity beam diameter along the b axis. |
| Applicability | Diagnostic | At 800 nm, hν ≈ 1.550 eV exceeds both the indirect and direct gaps. Ge is absorbing; the zero-dimensional Keldysh result is diagnostic only because linear one-photon absorption, the imaginary index, reflection, and propagation are omitted. |

γ = (ω/e)√(mᵣᵉ e c n ε₀ E_g / I), with ω = 2πc/λ. In the numerical evaluation, E_g is entered in eV and multiplied by e, while I is converted from W/cm² to W/m².

Reference result: ω = 2.354564e+15 rad/s and γ(I₀) = 1.610866 for I₀ = 1.00 × 10¹³ W/cm².

# The temporary value mᵣᵉ = 1.00 m₀ is retained by prior project decision for materials other than ZnS and ZnSe. γ scales as √mᵣᵉ, √E_g, √n, and I⁻¹ᐟ².

| Case | Input change | γ | Interpretation |
| --- | --- | --- | --- |
| Band-gap range | E_g = 0.66–0.8 eV | 1.6109–1.7735 | γ ∝ √E_g |
| Reduced mass | mᵣᵉ = 0.5, 1.0, 2.0 m₀ | 1.1391, 1.6109, 2.2781 | γ ∝ √mᵣᵉ |
| Index ±5% | n = 4.464–4.934 | 1.5701–1.6506 | γ ∝ √n |

Known Limitations

At 800 nm, hν ≈ 1.550 eV exceeds both the indirect and direct gaps. Ge is absorbing; the zero-dimensional Keldysh result is diagnostic only because linear one-photon absorption, the imaginary index, reflection, and propagation are omitted. The model also does not include avalanche ionization unless it is explicitly added by the associated code.

# Intensity Scan at the Reference Wavelength

| Peak intensity I | γ at 800 nm | Regime indicator |
| --- | --- | --- |
| 1e+12 W/cm² | 5.094004 | multiphoton-side (γ > 1) |
| 1e+13 W/cm² | 1.610866 | multiphoton-side (γ > 1) |
| 1e+14 W/cm² | 0.509400 | tunneling-side (γ < 1) |
| 1e+15 W/cm² | 0.161087 | tunneling-side (γ < 1) |

The table reports the Keldysh parameter for the same 800 nm material inputs over four peak intensities. F is surface fluence and a,b are the two measured 1/e² intensity beam diameters. They are recorded as experiment inputs but do not determine I in this sheet because pulse duration and the adopted spatiotemporal normalization are not specified.

# References and Traceability

G. E. Jellison Jr., Optical Materials 1, 151–160 (1992), DOI: 10.1016/0925-3467(92)90022-F (800 nm optical constants).

Ioffe Institute semiconductor database / standard room-temperature Ge band-gap data (band-gap context).

CODATA exact elementary charge and standard SI values for c, ε₀, and m₀.

Keldysh strong-field ionization convention as used in the existing project input documents; the associated script is the executable source for implementation details.

User-entered experiment fields F, a, and b were preserved from this document and copied into both parameter tables.

Values labeled provisional, proxy, interpolated, or not specified require source confirmation before quantitative interpretation.

Conclusion: the 800 nm inputs are internally consistent with the stated convention, but the resulting γ is a model diagnostic wherever ordinary optical absorption or uncertain material constants are important.