# KRS5 Keldysh Input Parameter Specification

Reference example at 800 nm; SI conversion is applied internally.

# Scope and Material Identity

Material: KRS-5 (TlBr–TlI mixed crystal). This sheet follows the BaF₂/NaCl input-document structure while retaining material-specific assumptions and limitations.

Parameter Status

# The reference calculation uses λ = 0.800 µm, I = 1.00 × 10¹³ W/cm², mᵣᵉ = 1.00 m₀, E_g = 2.5 eV (provisional placeholder; verify for the actual KRS-5 composition), and Re(n) = 2.49088.

| Symbol | Value | Unit | Definition / use | Status / source |
| --- | --- | --- | --- | --- |
| γ | 2.282608 | dimensionless | Keldysh parameter at I₀ | Calculated |
| c | 299792458 | m/s | Speed of light in vacuum | Exact SI |
| e | 1.602176634 × 10⁻¹⁹ | C | Elementary charge | Exact SI |
| ε₀ | 8.8541878128 × 10⁻¹² | F/m | Vacuum permittivity | Standard SI |
| mᵣᵉ | 1.00 | m₀ | Electron–hole reduced effective mass | Temporary project placeholder |
| n | 2.49088 | dimensionless | Real refractive index at 800 nm | n = 2.4909 at 0.800 µm is a Cauchy interpolation from tabulated KRS-5 values at 0.54, 1.00, and 1.50 µm; it is not a direct 800 nm measurement. No κ value is entered. |
| κ | not specified | dimensionless | Extinction coefficient at 800 nm | Not used in this zero-dimensional calculation |
| E_g | 2.5 | eV | Band-gap energy | provisional placeholder; verify for the actual KRS-5 composition |
| λ | 0.800 | µm | Vacuum wavelength | User-requested standard wavelength |
| ω | 2.354564e+15 | rad/s | Angular frequency, 2πc/λ | Calculated |
| I₀ | 1.00 × 10¹³ | W/cm² | Reference peak intensity | Independent scan input |
| F | Surface fluence | J/cm² | Surface fluence | User-supplied surface fluence; recorded as experiment input and not used to derive I in this sheet. |
| a | Beam-profile diameter along axis a | µm | Beam size along a | User-supplied 1/e² intensity beam diameter along the a axis. |
| b | Beam-profile diameter along axis b | µm | Beam size along b | User-supplied 1/e² intensity beam diameter along the b axis. |

800 nm lies within the nominal transmission range but near its short-wavelength side. The band gap and 800 nm extinction coefficient remain uncertain; the Re(n)-only, zero-dimensional result omits linear absorption, reflection, and propagation.

# Reproducible Calculation and Optical-Index Basis

n = 2.4909 at 0.800 µm is a Cauchy interpolation from tabulated KRS-5 values at 0.54, 1.00, and 1.50 µm; it is not a direct 800 nm measurement. No κ value is entered.

At 800 nm the photon energy is hν = 1.5498 eV. Optical constants and band-gap inputs must correspond to the actual sample temperature, composition, orientation, and batch whenever those variables are relevant.

Electric-field convention: E = √[2I/(c n ε₀)], so I = (1/2)c n ε₀E². The Keldysh expression below is kept consistent with the existing NaCl/BaF₂ documents and does not insert an additional factor of 2 into γ.

# Keldysh Parameter

| Input | Entered value | Implementation note |
| --- | --- | --- |
| Material | KRS-5 (TlBr–TlI mixed crystal) | Material-specific standalone input |
| λ | 0.800 µm | Used to calculate ω |
| n + iκ | 2.49088 + i(not specified) | Only Re(n) enters γ |
| E_g | 2.5 eV | provisional placeholder; verify for the actual KRS-5 composition |
| mᵣᵉ | 1.00 m₀ | Temporary project placeholder |
| I₀ | 1.00 × 10¹³ W/cm² | Converted to 1.00 × 10¹⁷ W/m² |
| F | Surface fluence J/cm² | User-supplied surface fluence; recorded as experiment input and not used to derive I in this sheet. |
| a | Beam-profile diameter along axis a µm | User-supplied 1/e² intensity beam diameter along the a axis. |
| b | Beam-profile diameter along axis b µm | User-supplied 1/e² intensity beam diameter along the b axis. |
| Applicability | Diagnostic | 800 nm lies within the nominal transmission range but near its short-wavelength side. The band gap and 800 nm extinction coefficient remain uncertain; the Re(n)-only, zero-dimensional result omits linear absorption, reflection, and propagation. |

γ = (ω/e)√(mᵣᵉ e c n ε₀ E_g / I), with ω = 2πc/λ. In the numerical evaluation, E_g is entered in eV and multiplied by e, while I is converted from W/cm² to W/m².

Reference result: ω = 2.354564e+15 rad/s and γ(I₀) = 2.282608 for I₀ = 1.00 × 10¹³ W/cm².

# The temporary value mᵣᵉ = 1.00 m₀ is retained by prior project decision for materials other than ZnS and ZnSe. γ scales as √mᵣᵉ, √E_g, √n, and I⁻¹ᐟ².

| Case | Input change | γ | Interpretation |
| --- | --- | --- | --- |
| Band-gap range | E_g = 2–3 eV | 2.0416–2.5005 | γ ∝ √E_g |
| Reduced mass | mᵣᵉ = 0.5, 1.0, 2.0 m₀ | 1.6140, 2.2826, 3.2281 | γ ∝ √mᵣᵉ |
| Index ±5% | n = 2.366–2.615 | 2.2248–2.3390 | γ ∝ √n |

Known Limitations

800 nm lies within the nominal transmission range but near its short-wavelength side. The band gap and 800 nm extinction coefficient remain uncertain; the Re(n)-only, zero-dimensional result omits linear absorption, reflection, and propagation. The model also does not include avalanche ionization unless it is explicitly added by the associated code.

# Intensity Scan at the Reference Wavelength

| Peak intensity I | γ at 800 nm | Regime indicator |
| --- | --- | --- |
| 1e+12 W/cm² | 7.218239 | multiphoton-side (γ > 1) |
| 1e+13 W/cm² | 2.282608 | multiphoton-side (γ > 1) |
| 1e+14 W/cm² | 0.721824 | tunneling-side (γ < 1) |
| 1e+15 W/cm² | 0.228261 | tunneling-side (γ < 1) |

The table reports the Keldysh parameter for the same 800 nm material inputs over four peak intensities. F is surface fluence and a,b are the two measured 1/e² intensity beam diameters. They are recorded as experiment inputs but do not determine I in this sheet because pulse duration and the adopted spatiotemporal normalization are not specified.

# References and Traceability

KRS-5 refractive-index table: n = 2.68059 at 0.54 µm, 2.44620 at 1.00 µm, and 2.40774 at 1.50 µm (basis of the stated Cauchy interpolation).

The 2.50 eV band gap is retained as a provisional placeholder and must not be treated as a verified material constant.

CODATA exact elementary charge and standard SI values for c, ε₀, and m₀.

Keldysh strong-field ionization convention as used in the existing project input documents; the associated script is the executable source for implementation details.

User-entered experiment fields F, a, and b were preserved from this document and copied into both parameter tables.

Values labeled provisional, proxy, interpolated, or not specified require source confirmation before quantitative interpretation.

Conclusion: the 800 nm inputs are internally consistent with the stated convention, but the resulting γ is a model diagnostic wherever ordinary optical absorption or uncertain material constants are important.