# Keldysh Parameter of NaCl: Formula, Symbol Values, and Review Sources

Reference example at 800 nm and a peak intensity of 1.00×10¹³ W/cm² — review draft

# 1. Formula and Interpretation

γ = (ω/e) √[(mᵣ e c n ε₀ E_g)/I]

Here, E_g is entered in eV, and the factor e converts it to joules; I must be expressed in W/m². This document and the script follow the source-paper convention E = √[I/(cnε₀)], so γ contains I, not 2I, in the denominator. The Keldysh parameter γ is dimensionless. In general, γ ≫ 1 indicates a multiphoton-ionization (MPI) dominated regime, γ ≪ 1 indicates a tunneling-ionization (TI) dominated regime, and γ ≈ 1 represents the transition region.

# 2. Numerical Value, Range, and Source for Every Symbol

| Symbol | Meaning | Value or Range Used for NaCl | Unit | Source and Review Note |
| --- | --- | --- | --- | --- |
| γ | Keldysh parameter | Reference value: 3.30; combined sensitivity range: 2.27–4.81 | Dimensionless | Calculated from the review inputs below. The range combines mᵣ = 0.5–2.0 m₀ and E_g = 8.0–9.0 eV; it is not directly measured. |
| ω | Laser angular frequency, ω = 2πc/λ | 2.35456×10¹⁵ | rad·s⁻¹ | Calculated from λ = 800 nm and the exact value of c. |
| e | Elementary charge | 1.602176634×10⁻¹⁹ | C | Exact SI-defined value; NIST CODATA. |
| mᵣ | Electron–hole reduced effective mass | Temporary project input: 1.000 m₀ = 9.10938×10⁻³¹; sensitivity range: 0.5–2.0 m₀ | kg | Temporary project input. Do not treat m₀ or the range as a measured NaCl reduced mass; choose band-specific mₑ* and mₕ* before final input. |
| c | Speed of light in vacuum | 299792458 | m·s⁻¹ | Exact SI-defined value; NIST CODATA. |
| n | NaCl refractive index (297 K, 800 nm) | 1.53560 | Dimensionless | Calculated from Li’s evaluated NaCl dispersion relation; nominal validity range 0.20–30 μm at 297 K. |
| ε₀ | Vacuum permittivity | 8.8541878188×10⁻¹² | F·m⁻¹ | NIST CODATA recommended value. |
| E_g | NaCl electronic band gap | Reference: 8.5; review range: 8.0–9.0 | eV | 8.5 eV is a historical electronic-gap reference. Optical-gap values can be lower; confirm the gap definition used by the intended Keldysh model. |
| I | Peak laser intensity | Reference: 1.00×10¹³ W/cm² = 1.00×10¹⁷ W/m²; example range: 10¹²–10¹⁵ W/cm² | W/m² | Experimental input, not a NaCl material constant. Use the spatiotemporal peak intensity, not average power divided by area. |
| F₀ | Peak fluence | 0.392289 | J/cm² | Elliptical-Gaussian peak fluence calculated from E = 150 µJ and F₀ = 2E/(πab), where a and b are 1/e² intensity radii (half of the full 1/e² intensity diameters). |
| a | 1/e² intensity radius along the first principal axis | 113.3 | µm | 1/e² intensity radius; half of the measured full 1/e² intensity diameter. |
| b | 1/e² intensity radius along the second principal axis | 214.85 | µm | 1/e² intensity radius; half of the measured full 1/e² intensity diameter. |
| λ | Laser vacuum wavelength | 800 nm = 8.00×10⁻⁷ m | m | Experimental input; this review example uses the Ti:sapphire fundamental wavelength. |
| m₀ | Free-electron rest mass | 9.1093837139×10⁻³¹ | kg | NIST CODATA recommended value, used to express effective-mass ratios. |

# 3. Reproducible Calculation of the NaCl Refractive Index

Li critically evaluated the refractive index of alkali halides and gives a dispersion formula for NaCl at 297 K over 0.20–30 μm:

n² − 1 = 0.00055 + 0.19800λ²/(λ²−0.050²) + 0.48398λ²/(λ²−0.100²) + 0.38696λ²/(λ²−0.128²) + 0.25998λ²/(λ²−0.158²) + 0.08796λ²/(λ²−40.50²) + 3.17064λ²/(λ²−60.98²) + 0.30038λ²/(λ²−120.34²)

Here, λ is expressed in μm. Substituting λ = 0.800 μm gives n = 1.535596; the tables report 1.53560. This is a 297 K bulk-crystal value; confirm the temperature, sample composition, and wavelength before using it as a code input.

# 4. Reference Numerical Calculation

| Parameter | Reference Value | Note |
| --- | --- | --- |
| λ | 800 nm | Specified review condition |
| ω | 2.35456×10¹⁵ rad·s⁻¹ | From 2πc/λ |
| n | 1.53560 | Li evaluated dispersion relation at 297 K |
| E_g | 8.5 eV | Electronic-gap convention; confirm against model choice |
| mᵣ | 1.000 m₀ | Temporary project input; not a uniquely measured NaCl value |
| I | 1.00×10¹³ W/cm² | Specified peak intensity |
| F₀ | 0.392289 J/cm² | Elliptical-Gaussian peak fluence calculated from E = 150 µJ and F₀ = 2E/(πab), where a and b are 1/e² intensity radii (half of the full 1/e² intensity diameters). |
| a | 113.3 µm | 1/e² intensity radius; half of the measured full 1/e² intensity diameter. |
| b | 214.85 µm | 1/e² intensity radius; half of the measured full 1/e² intensity diameter. |
| γ | 3.30 | MPI regime (review calculation) |

Calculated review result: γ = 3.30. This value temporarily uses mᵣ = m₀ as the project input, not as a measured NaCl reduced effective mass. Under the commonly used interpretation, this reference condition is closer to the MPI-dominated regime. Because γ ∝ √mᵣ, γ ∝ √E_g, and γ ∝ I⁻¹ᐟ², the reduced effective mass and the actual peak laser intensity are the key inputs to verify before calculation.

# 5. Sensitivity to Effective-Mass Uncertainty

| Assumed mᵣ | E_g Range (eV) | γ Range | Interpretation |
| --- | --- | --- | --- |
| 0.5 m₀ | 8.0–9.0 | 2.27–2.41 | MPI |
| 1.0 m₀ | 8.0–9.0 | 3.20–3.40 | MPI |
| 2.0 m₀ | 8.0–9.0 | 4.53–4.81 | MPI |

Important review note: the range 0.5–2.0 m₀ in the table is a calculation interval used to demonstrate model sensitivity; it is not a reported NaCl electron–hole reduced effective mass. The Keldysh expression requires mᵣ = (mₑ* mₕ*)/(mₑ* + mₕ*). A material- and band-extremum-specific effective-mass source should be selected before this draft is used as a final simulation input. Until then, this project temporarily uses mᵣ = 1.0m₀.

# 6. Intensity Scan (Temporary project input mᵣ = m₀ and E_g = 8.5 eV)

| Peak Intensity (W/cm²) | γ | Indicative Regime |
| --- | --- | --- |
| 1×10¹² | 10.45 | MPI |
| 1×10¹³ | 3.30 | MPI |
| 1×10¹⁴ | 1.05 | Transition region |
| 1×10¹⁵ | 0.330 | TI |

# 7. References

• Li, H. H. (1976). Refractive index of alkali halides and its wavelength and temperature derivatives. Journal of Physical and Chemical Reference Data, 5, 329–528. Evaluated NaCl dispersion data and the 297 K formula used here.

• Poole, R. T., Liesegang, J., Leckey, R. C. G., & Jenkin, J. G. (1975). Electronic band structure of the alkali halides. II: Critical survey of theoretical calculation. Physical Review B, 11, 5194. Historical reference for an approximately 8.5 eV electronic gap for NaCl.

• Franchini, C., et al. (2018). Band-edge levels of the NaCl(100) surface: Self-consistent hybrid density functional theory compared to many-body perturbation theory. Physical Review B, 97, 235447. Notes bulk optical gaps near 7.7–7.9 eV and shows why the gap definition must be selected deliberately.

• NIST CODATA recommended values of the fundamental physical constants: e, c, ε₀, and m₀.

Concluding review note: this document uses the 8.5 eV electronic-gap convention only as a transparent reference input. NaCl literature also reports lower optical-gap values depending on the experimental observable. Before a final Keldysh calculation, confirm the chosen gap definition, wavelength, temperature, actual peak intensity, and a defensible electron–hole reduced effective mass for the exact NaCl sample.