# Keldysh Parameter of Ti:Sapphire: Formula, Symbol Values, and Reliable Sources

Reference example at 800 nm and a peak intensity of 1.00×10¹³ W/cm²

# 1. Formula and Interpretation

γ = (ω/e) √[(mᵣ e c n ε₀ E_g)/I]

Here, E_g is entered in eV, and the factor e converts it to joules; I must be expressed in W/m². This document and the script follow the source-paper convention E = √[I/(cnε₀)], so γ contains I, not 2I, in the denominator. The Keldysh parameter γ is dimensionless. The Ti:Sapphire result is a diagnostic host-material reference, not a dopant-resolved propagation model.

# 2. Numerical Value, Range, and Source for Every Symbol

| Symbol | Meaning | Value or Range Used for Ti:Sapphire | Unit | Source and Cautionary Note |
| --- | --- | --- | --- | --- |
| γ | Keldysh parameter | Reference value: 3.60; mass-sensitivity range: 2.52–5.12 | Dimensionless | Calculated from the parameters below using the source-paper convention E = √[I/(cnε₀)]. The range is a sensitivity interval for mᵣ = 0.5–2.0 m₀; it is not a directly measured material constant. |
| ω | Laser angular frequency, ω = 2πc/λ | 2.35456×10¹⁵ | rad·s⁻¹ | Calculated from λ = 800 nm and the exact value of c. |
| e | Elementary charge | 1.602176634×10⁻¹⁹ | C | Exact SI-defined value; NIST CODATA. |
| mᵣ | Electron–hole reduced effective mass | Temporary project input: 1.000 m₀ = 9.10938×10⁻³¹; sensitivity range: 0.5–2.0 m₀ | kg | A band-specific Ti:Sapphire electron–hole reduced mass is not fixed here. The 1.0m₀ value is a temporary project input and the range is a declared sensitivity interval. |
| c | Speed of light in vacuum | 299792458 | m·s⁻¹ | Exact SI-defined value; NIST CODATA. |
| nₒ | Ordinary sapphire refractive index (800 nm) | 1.760 | Dimensionless | Room-temperature ordinary-polarization input. Use nₑ for the specified extraordinary polarization instead. |
| ε₀ | Vacuum permittivity | 8.8541878188×10⁻¹² | F·m⁻¹ | NIST CODATA recommended value. |
| E_g | α-Al₂O₃ host band gap | Reference: 8.8 | eV | Host-material reference. Ti³⁺ impurity bands and gain are separate, sample-dependent optical inputs. |
| I | Peak laser intensity | Reference: 1.00×10¹³ W/cm² = 1.00×10¹⁷ W/m²; example range: 10¹²–10¹⁵ W/cm² | W/m² | Experimental input, not a material constant. Use spatiotemporal peak intensity. |
| F₀ | Peak fluence | 0.61 | J/cm² | Experimental input; left blank because no fluence is specified. |
| a | 1/e² intensity radius along the first principal axis | 162.1 | µm | Experimental 1/e² intensity radius; left blank because it is not specified. If supplied from a diameter, use half of the full 1/e² intensity diameter. |
| b | 1/e² intensity radius along the second principal axis | 152.4 | µm | Experimental 1/e² intensity radius; left blank because it is not specified. If supplied from a diameter, use half of the full 1/e² intensity diameter. |
| λ | Laser vacuum wavelength | 800 nm = 8.00×10⁻⁷ m | m | Experimental input; a common Ti:Sapphire reference wavelength. |
| m₀ | Free-electron rest mass | 9.1093837139×10⁻³¹ | kg | NIST CODATA recommended value, used to express effective-mass ratios. |

# 3. Reproducible Ti:Sapphire Refractive-Index Input

Tapping and Reilly measured the ordinary refractive index of sapphire at 799 nm from 24 to 1060 °C. Their fitted room-temperature value is nₒ ≈ 1.760. This document uses nₒ = 1.760 for an ordinary-polarized 800 nm field.

Ti:sapphire is birefringent. A commonly tabulated extraordinary value near 800 nm is nₑ ≈ 1.752; replace nₒ with the index appropriate to the crystal cut and polarization. The ordinary/extraordinary distinction changes γ only weakly, but it should still be stated in the simulation input.

The 800 nm photon energy is 1.550 eV, well below the α-Al₂O₃ host band gap used here (8.8 eV); the nominal photon order is 5.68, hence six photons at zero field. Ti³⁺ doping supplies broad absorption/emission bands, so the dopant concentration, inversion, and crystal orientation must be recorded separately when modeling propagation or gain.

# 4. Reference Numerical Calculation

| Parameter | Reference Value | Note |
| --- | --- | --- |
| λ | 800 nm | Specified |
| ω | 2.35456×10¹⁵ rad·s⁻¹ | From 2πc/λ |
| nₒ | 1.760 | Ordinary index near 799–800 nm |
| E_g | 8.8 eV | α-Al₂O₃ host-gap reference |
| mᵣ | 1.000m₀ | Temporary project input, not a measured Ti:Sapphire reduced mass |
| I | 1.00×10¹³ W/cm² | Specified peak intensity |
| F₀ | 0.61 | Experimental input; left blank because no fluence is specified. |
| a | 162.1 | Experimental 1/e² intensity radius; left blank because it is not specified. If supplied from a diameter, use half of the full 1/e² intensity diameter. |
| b | 152.4 | Experimental 1/e² intensity radius; left blank because it is not specified. If supplied from a diameter, use half of the full 1/e² intensity diameter. |
| γ | 3.60 | MPI-side diagnostic reference calculation |

Calculated reference result: γ = 3.60 using the source-paper convention E = √[I/(cnε₀)]. This is MPI-side under the common Keldysh interpretation. It temporarily uses mᵣ = m₀ as the project input, not as a measured Ti:Sapphire electron–hole reduced effective mass.

# 5. Sensitivity to Effective-Mass Uncertainty

| Assumed mᵣ | E_g Range (eV) | γ Range | Interpretation |
| --- | --- | --- | --- |
| 0.5m₀ | 8.6–8.9 | 2.52–2.56 | MPI-side sensitivity interval |
| 1.0m₀ | 8.6–8.9 | 3.56–3.62 | MPI-side sensitivity interval |
| 2.0m₀ | 8.6–8.9 | 5.03–5.12 | MPI-side sensitivity interval |

Important review note: no single, verified bulk electron–hole reduced effective mass was identified for Ti³⁺:Al₂O₃ that can be inserted universally into this Keldysh expression. The range 0.5–2.0m₀ is a transparent calculation interval, not a material-property claim. If a band-structure calculation or measurement supplies mₑ* and mₕ*, replace this interval with mᵣ = (mₑ*mₕ*)/(mₑ*+mₕ*).

# 6. Intensity Scan (Temporary project input mᵣ = m₀ and E_g = 8.8 eV)

| Peak Intensity (W/cm²) | γ | Indicative Regime |
| --- | --- | --- |
| 1×10¹² | 11.38 | MPI |
| 1×10¹³ | 3.60 | MPI |
| 1×10¹⁴ | 1.14 | MPI/transition side |
| 1×10¹⁵ | 0.360 | TI |

# 7. References

• Tapping, J., & Reilly, M. L. (1986). Index of refraction of sapphire between 24 and 1060 °C for wavelengths of 633 and 799 nm. Journal of the Optical Society of America A, 3, 610–616. Source for the ordinary sapphire index near 800 nm.

• NASA Technical Publication 2020-220002, radiation-effects materials-property compilation. Lists the α-Al₂O₃ (sapphire) band gap as 8.8 eV. This host-gap value is used for the Ti:sapphire strong-field reference calculation.

• Moulton, P. F. (1986). Spectroscopic and laser characteristics of Ti:Al₂O₃. Journal of the Optical Society of America B, 3, 125–133. Standard reference for Ti:sapphire absorption/emission and laser-material behavior.

• National Academies of Sciences, Engineering, and Medicine (2018). Opportunities in Intense Ultrafast Lasers. Ti:sapphire systems operate around a central wavelength of 800 nm; actual spectrum, pulse duration, and peak intensity are experiment-specific inputs.

• NIST CODATA recommended values of the fundamental physical constants: e, c, ε₀, and m₀.

Concluding input note: nₒ = 1.760, E_g = 8.8 eV, and λ = 800 nm form a traceable Ti:sapphire host-material reference. The reduced mass is the principal unresolved material input in this simplified model. Before using the calculation for a specific crystal, replace the reference mᵣ assumption with band-specific data and specify Ti concentration, temperature, orientation, polarization, pulse duration, and peak intensity.