# Keldysh Parameter of BaF₂: Formula, Symbol Values, and Reliable Sources

Reference example at 800 nm and a peak intensity of 1.00×10¹³ W/cm²

# 1. Formula and Interpretation

γ = (ω/e) √[(mᵣ e c n ε₀ Eg)/I]

Here, E_g is entered in eV, and the factor e converts it to joules; I must be expressed in W/m². The Keldysh parameter γ is dimensionless. In general, γ ≫ 1 indicates a multiphoton-ionization (MPI) dominated regime, γ ≪ 1 indicates a tunneling-ionization (TI) dominated regime, and γ ≈ 1 represents the transition region.

# 2. Numerical Value, Range, and Source for Every Symbol

| Symbol | Meaning | Value or Range Used for BaF₂ | Unit | Source and Cautionary Note |
| --- | --- | --- | --- | --- |
| γ | Keldysh parameter | Reference value: 3.61; mass-sensitivity range: 2.54–5.20 | Dimensionless | Calculated from the parameters below. The range corresponds to mᵣ = 0.5–2.0 m₀ and E_g = 10.5–11.0 eV; it is not a directly measured quantity. |
| ω | Laser angular frequency, ω = 2πc/λ | 2.35456×10¹⁵ | rad·s⁻¹ | Calculated from λ = 800 nm and the exact value of c. |
| e | Elementary charge | 1.602176634×10⁻¹⁹ | C | Exact SI-defined value; NIST CODATA. |
| mᵣ | Electron–hole reduced effective mass | Reference: 1.000 m₀ = 9.10938×10⁻³¹; sensitivity range: 0.5–2.0 m₀ | kg | A reliable BaF₂ hole effective mass is not consistently constrained by experiment, so no unique mᵣ can be cited rigorously. An electron effective mass m* ≈ 2m₀ has been used in a BaF₂ electron-thermalization model; the interval 0.5–2.0 m₀ is retained only for sensitivity analysis and is not claimed to be a measured BaF₂ constant. |
| c | Speed of light in vacuum | 299792458 | m·s⁻¹ | Exact SI-defined value; NIST CODATA. |
| n | BaF₂ refractive index (25 °C, 800 nm) | 1.47040 | Dimensionless | Calculated from Malitson’s Sellmeier equation for BaF₂; original measurement range: 0.2652–10.346 μm. |
| ε₀ | Vacuum permittivity | 8.8541878188×10⁻¹² | F·m⁻¹ | NIST CODATA recommended value. |
| E_g | BaF₂ band gap | Reference: 10.6; cautious range: 10.5–11.0 | eV | Experimental and spectroscopic literature commonly reports approximately 10.5–11 eV; 10.6 eV is a representative room-temperature value. |
| I | Peak laser intensity | Reference: 1.00×10¹³ W/cm² = 1.00×10¹⁷ W/m²; example range: 10¹²–10¹⁵ W/cm² | W/m² | Experimental input, not a BaF₂ material constant. For pulsed lasers, use the spatiotemporal peak intensity rather than average power divided by area. |
| λ | Laser vacuum wavelength | 800 nm = 8.00×10⁻⁷ m | m | Experimental input; a common example for the Ti:sapphire fundamental wavelength. |
| m₀ | Free-electron rest mass | 9.1093837139×10⁻³¹ | kg | NIST CODATA recommended value, used to express effective-mass ratios. |

# 3. Reproducible Calculation of the BaF₂ Refractive Index

Malitson measured the refractive index of BaF₂ at 25 °C over the wavelength range 0.2652–10.346 μm and reported:

n² − 1 = 0.643356 λ²/[λ² − (0.057789)²] + 0.506762 λ²/[λ² − (0.10968)²] + 3.8261 λ²/[λ² − (46.3864)²]

Here, λ is expressed in μm. Substituting λ = 0.800 μm gives n = 1.470395; the tables report 1.47040. This value is more traceable than simply stating “approximately 1.47.”

# 4. Reference Numerical Calculation

| Parameter | Reference Value | Note |
| --- | --- | --- |
| λ | 800 nm | Specified |
| ω | 2.35456×10¹⁵ rad·s⁻¹ | From 2πc/λ |
| n | 1.47040 | Malitson Sellmeier equation |
| E_g | 10.6 eV | Representative literature value |
| mᵣ | 1.000 m₀ | Reference assumption; not a uniquely measured BaF₂ value |
| I | 1.00×10¹³ W/cm² | Specified peak intensity |
| γ | 3.61 | MPI regime |

Calculated result: γ = 3.61. Under the commonly used interpretation, this reference condition is closer to the MPI-dominated regime. Because γ ∝ √mᵣ, γ ∝ √E_g, and γ ∝ I⁻¹ᐟ², the largest uncertainty usually arises from the reduced effective mass and the actual peak laser intensity.

# 5. Sensitivity to Effective-Mass Uncertainty

| Assumed mᵣ | E_g Range (eV) | γ Range | Interpretation |
| --- | --- | --- | --- |
| 0.5 m₀ | 10.5–11.0 | 2.54–2.60 | MPI |
| 1.0 m₀ | 10.5–11.0 | 3.59–3.68 | MPI |
| 2.0 m₀ | 10.5–11.0 | 5.08–5.20 | MPI |

Important: the range 0.5–2.0 m₀ in the table is a calculation interval used to demonstrate model sensitivity. Published work has used an electron effective mass of approximately 2m₀ in BaF₂ modeling; however, the Keldysh expression strictly requires the electron–hole reduced effective mass, mᵣ = (mₑ* mₕ*)/(mₑ* + mₕ*). Without a reliable hole effective mass, 2m₀ should not be reported as a known reduced effective mass of BaF₂.

# 6. Intensity Scan (Reference mᵣ = m₀ and E_g = 10.6 eV)

| Peak Intensity (W/cm²) | γ | Indicative Regime |
| --- | --- | --- |
| 1×10¹² | 11.42 | MPI |
| 1×10¹³ | 3.61 | MPI |
| 1×10¹⁴ | 1.14 | Transition region |
| 1×10¹⁵ | 0.361 | TI |

# 7. References

• Malitson, I. H. (1964). Refractive properties of barium fluoride. Journal of the Optical Society of America, 54(5), 628–632. Source for the BaF₂ refractive-index measurements and Sellmeier equation.

• Andrade, A. B., et al. (2017). Particle size effects on structural and optical properties of BaF₂. RSC Advances, 7. Reports a BaF₂ optical band gap of approximately 10.5 eV.

• Chen, J., et al. (2002). The electronic structure of color centers in BaF₂. Nuclear Instruments and Methods in Physics Research B. Reports a calculated band gap of approximately 10.6 eV, consistent with the established experimental range.

• Arimoto, O., et al. (1998). Nonlinear spectroscopy of BaF₂ valence excitons. Radiation Effects and Defects in Solids. Describes BaF₂ as a wide-band-gap material with a gap of approximately 11 eV.

• Vistovskyy, V. V., et al. (2013). Self-trapped exciton and core-valence luminescence in BaF₂ nanoparticles. Journal of Applied Physics, 114, 194306. Uses m* ≈ 2m₀ in an electron-thermalization estimate; this is not a direct measurement of the electron–hole reduced mass.

• NIST CODATA recommended values of the fundamental physical constants: e, c, ε₀, and m₀.

Concluding note: apart from the fundamental constants, λ and I are experimental conditions; n depends on wavelength and temperature; E_g may vary slightly with measurement method, temperature, and sample condition; and mᵣ is the parameter that requires the greatest caution. For formal publication, preference should be given to a first-principles or experimentally determined effective mass that matches the sample, crystal direction, and relevant band extrema.