Combined photoionization and avalanche ionization rates;

∂ne∂t=WPIIt+WAVItne(t)                                                                     (2)

where WPI and WAV are the photoionization and avalanche ionization rates, respectively, ne is the free electron density, and It is the instantaneous laser intensity. WPI is expressed as

WPI=4ω9πωmerℏγ11.5Qγ,x×exp-π×x+1Kγ1-Mγ1Mγ2                      (3)

where Qγ,x=π2Kγ2j=0∞exp-πjKγ1-Mγ1Mγ2×∅πx+1-x+j2Kγ2Mγ2,

γ1=γ1+γ2, γ2=11+γ2, ∅x=e-x20xet2dt, x=2EgMγ2πℏωγ1.

Here, K and M are elliptic integrals of the first and second kind, respectively, mer is the electron reduced mass, x is the effective bandgap, ∅xis the Dawson function, and ℏ is the reduced Planck’s constant.

The impact ionization is described by the Drude model and is expressed as

WAV=σEgI(t)                                                              (4)

where σ  is the single-photon absorption cross-section

σ=e2cε0men0τc1+ω2τC2                                                      (5)

Here, τc is the collision time given as

τc=16πε02m(0.1Eg)32e4ne(t)                                                         (6)

================ Density-growth summary ================

| Case | lambda(um) | I0(W/cm2) | n_photo(cm-3) | n_av_added(cm-3) | n_total(cm-3) |
| --- | --- | --- | --- | --- | --- |
| ZnSe_NIR | 0.8 | 1.0522e+12 | 4.2925e+20 | 8.3139e+20 | 1.2606e+21 |
| ZnS_NIR | 0.8 | 1.5970e+12 | 1.7118e+19 | 2.5055e+20 | 2.6767e+20 |
| ZnSe_LWIR | 9.2 | 3.8987e+11 | 1.1290e+18 | 5.6853e+21 | 5.6864e+21 |
| ZnS_LWIR | 9.2 | 5.5897e+11 | 1.5994e+15 | 2.7382e+14 | 1.8733e+15 |

Additional plots

- NIR

Dependence of peak ionization rates and electron density on the laser intensity.

At lower laser intensities, photoionization (WPI) dominates, and the electron density is not enough for avalanche (time for avalanche (Eq. 6, collision time reduces as 1/ne) exceeds the pulse duration). The absorption cross-section increases with the reduction of collision time (Eq. 5). Thus, the impact ionization rate (WAV) shows linear dependence with laser intensity (Eq. 4). The total ionization rate (Wtotal) coincides with photoionization.

At higher intensities, the collision time gets shorter, and the absorption cross-section reaches a maximum at 1/τc= ω. The WAV dependence on laser intensities becomes nonlinear, and there is a strong feedback between ne and WAV which becomes explosive at 1/τc= ω, resulting in step-wise increase in neand the total ionization rate (Wtotal). The step-wise increase also characterizes a transition from a photoionization-dominated mechanism to an impact ionization-dominated mechanism taking place at some threshold intensity Ith, when WPI (Ith)= WAV (Ith).

- LWIR

At lower intensities, photoionization dominates.

At higher intensities, the stepwise increase in the ionization rate and electron density appears more rapid than in the NIR case, i.e., the step occurs over a smaller range of intensities.

Can the threshold intensities at the initiation of step-wise increase of electron densities be associated with LIDT?

- NIR and LWIR comparison

The vertical dashed lines correspond to the intensities at the measured LIDTs: NIR (right line), LWIR (left line).